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Company Information

	Poducer
	:
	STİL TRAFİK İŞARETLERİ SAN. VE TİC. A.Ş.

	Address
	:
	Kuştepe Mah. Leylak 1 Sokak No:3 Murat İş Merkezi B Blok K:12 D:41 Şişli İstanbul

	Phone/Fax
	:
	+90 212 491 01 44  /  +90 212 533 79 64

	Web/E-mail
	:
	www.stiltrafik.com  /  info@stiltrafik.com 


Product
Product name	: LineStil Alkyd Road Marking Paint (Sovent Based)
Color		: White – Yellow 
Usage Area	: Bituminous asphalt roads and concrete surfaces for marking
Product Description

LineStil Alkyd Road Marking Paint is a one-component, fast-drying, solvent-based road marking paint containing specially modified high-performance alkyd-based resin with good physical and chemical resistance, adhesion and abrasion resistance
When solvent-based road marking paints are applied by brush, roller and spray method, they form a film by evaporation of volatile organic solvents  in the paint and/or chemically. It is designed for use on asphalt bituminous roads and concrete surfaces.
LineStil Alkyd Road marking paint meets the requirements of the General Directorate of Highways Technical Specifications (Turkiye), TS EN 1871 and TS EN 1436 standards.

CHARACTERISTICS
· Excellent adhesion. 
· High mechanical and chemical resistance
· UV resistance
· Fast drying, better durability, better color retention and luminance
· High coverage and reflectivity.
· Hydrophobic surface with self-cleaning feature.
· Higher quality resulting from the fastest drying time among road marking paints (suitable ambient and surface temperature, humidity environment). After the application, according to the surface temperatures specified in the table below, depending on the drying times, the application area can be opened to traffic.
· Providing excellent resistance to bleeding on 
· Easy to handle with all marking machines and spray equipment, even at high ambient temperature.
Application

Surface Preparation Information
LineStil Alkyd Road Marking Paint performance varies depending on the preparation level of the surface to be applied. The application surface must be clean, dry, dust-free, free of oil and other surface residues and loose materials via compressed air, broom, vacuum cleaner, water jet. The surface to be applied should not be wet in any way. All auxiliary equipment for surface cleaning should be available before application. Center line or sideline pre-markings and points on the road should be pre-marked using rope, chalk or any pre-marking method on newly installed asphalt roads. The temperature of the paint should be 5 °C higher than the road surface to be applied.

Application Surface
It is suitable for asphalt surfaces and bitumen substrates. 
Weather Condition
For a correct application ; ambient temperature, substrate temperature, humidity and subsequent application is very important in weather conditions Always check the weather forecast and do not start the application if heavy rain is expected within 2 hours. Application ambient temperature should be the range of 5 °C and 40 °C. After a homogeneous mixture is prepared, it is applied with the help of suitable equipment for the surface. The main parameters that will affect the drying time are low air temperature, low ground temperature, high relative humidity, dew and also rain. According to the ambient temperature and relative humidity 50% specified in the table below, the application area can be opened to traffic, taking into account the drying times.


	Drying Time (Relative Humidity 50%) at certain temperature
	10 °C
	23 °C
	40 °C

	Substrate Touch Dry
	20 min
	10 min
	7 min

	Hard Dry
	60 min
	30 min
	15 min

	Overcoating (Minimum)
	120 min
	60 min
	30 min




Paint Selection and Safety
It is preferable to use only the recommended or specified paint for each application. Avoid keeping and storing indoors and outdoors for a long time as much as possible. The paints should be mixed homogeneously and applied, in order to achieve high performance in the application. Make sure lids are tightly closed during transport of buckets / pallets or when storing products to avoid spillage, fire risk and solvent evaporation. Keep away from heat and flame. Please use suitable protective equipment, gloves and mask and refer to MSDS and / or labels for more safety procedures.

Application Equipment
It is recommended to apply with professional application team. And also can be applied successfully with airless or air assist spray application equipment. The appropriate film thickness anf width are obtained by adjusting the height of the spray gun, nozzle diameter, air pressure and driving speed. It can be applied successfully with a brush or roller for small applications.

Paint Preparation
Before application, it is mixed with a mixer until it reaches a homogeneous consistency. The paint is made ready for application. It is recommended to practice with a professional team.
Caution: It is recommended that the process be carried out in an open and well ventilated environment in order to avoid sparking due to the electric mixer used..

Application Condition
	Temperature
	:
	5 - 40 °C

	Relative Humidity
	:
	80% (max).

	Drying Time
	:
	23 min (15 °C temp. & 50% humudity)




Glass Beads Usage Amounts
	Wet Film Thickness [µ]
	Dry Film Thickness [µ]
	Consumption [kg / m²]

	140
	80
	0,25

	175
	100
	0,30

	263
	150
	0,45

	307
	175
	0,50

	
Note: The values given in the table are theoretical. Consumption amount may vary depending on the application surface and ambient condition.


	Glass Beads ( TS EN 1423 )
	Ratio
	Consumption

	
	265 g/m²
	350 g/m²



Day&Night Visibility
Night Visibility: Due to the glass beads in different sizes on the road markings, the light beams from the vehicle headlights are reflected back. This results in "lighting" the lane, which creates night visibility, a decisive plus for road safety Visibility increases according to the degree of embedding of the glass beads in the road marking paint and the size, quantity and quality.
Daytime Visibility: The contrast between the coating and the pigmentation of the marking material allows the stripes to be clearly seen in daylight conditions.

Physical Properties
	COLOR
	WHITE
	YELLOW

	VISCOSITY (DANIEL)
	80-95 KU
	80-95 KU

	DENSITY
	1,60 g/ml ± 0,10
	1,60 g/ml ± 0,10

	LUMINANCE CLASS / BRIGHTNESS FACTOR
	LF7 / β ≥ 0,85
	LF2 / β ≥ 0,50

	AMOUNT OF SOLID MATERIAL
	%75 ± 2
	%75 ± 2

	
	
	

	The Difference Classes in Luminosity Factor After UV Aging Test

	COLOR
	CLASS
	∆β

	WHITE, YELLOW
	UV-1
	≤0,05

	
	
	

	The Difference Classes in Luminosity Factor After Bleeding Resistance Test

	RENK
	CLASS
	∆β

	WHITE, YELLOW
	BR-1
	≤0,03



Waste Procedure
All regulations regarding the transportation, storage and disposal of all hazardous materials and wastes should  be followed carefully. Paint pail and related materials should be insulated in accordance with the required waste regulations. Otherwise, it may result in penalties specified in the legal regulations. Please follow all regulations and minimize the excessive usage as possible. 

Storage
Store between 5 °C and 30 °C in closed areas keeping away from direct sunlight. The storage area should be adequately ventilated to prevent moisture build-up. The storage area should be adequately ventilated to prevent moisture build-up. The lid should be tightly closed when the paint pail is not used. The shelf life of LineStil Alkyd Road Marking Paint is minimum 1 year in its original packaging and under suitable storage conditions.

Packaking
LineStil Alkyd Road Marking Paint is produced in 25 kg metal cans as standard and also can be produced in 180 kg barrels and 1000 kg IBC packages upon request.

Important Information
The information given in this data sheet is not intended to be comprehensive and may not be used for any purpose other than that specifically recommended on this sheet without our written approval as to the suitability of the product for its intended use. Otherwise, it is entirely user's own responsibility. As conditions of use, application method and surface suitability during painting are out of our control. The recommendations contained herein do not make any guarantees. The recommendations contained herein do not give any guarantee. Therefore, we accept no responsibility whatsoever for any loss or damage caused by the performance or the use of this product. The information on this data sheet is obliged to make changes from time to time in the light of experience and ongoing product development programs. It is the user's responsibility to ensure that this page is up-to-date before using the product.

Note: These data have been tested under lab conditions in the R&D department of Stil Trafik İşaretleri San. Ve Tic. A.Ş. Our company cannot be held responsible for any direct, indirect, special and consequential losses and damages that may arise from relying on this information and its use.
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